S1 Average Crystal size (nm) of adsorbents before and after (Fe2+) ion removal.

| Character | Average crystal size (nm) before removal (Fe2+) ions | Average crystal size (nm) after removal (Fe2+) ions |
| --- | --- | --- |
| DCP | 47 | 48 |
| (DCP – CS1) | 41 | 42 |
| (DCP – CS2) | 32 | 44 |

S2 IR spectra λ (cm-1) and assignments for adsorbents after removal (Fe2+) ions.

| (DCP) + Fe2+ | (DCP-CS1) + Fe2+ | (DCP-CS2) + Fe2+ | Assignments |
| --- | --- | --- | --- |
| 3447.46 | 3443.07 | 3443.50 | O–H stretching of residual free water |
| 2925.37 2857.41 | 2956.93 2924.02 2853.80 | 2960.66 2924.67 2854.29 | (P) O–H stretching |
| 1639.05 | 1630 | 1630 | H –O–H bending and rotation of residual free water |
| - | 1638.04 | 1645.02 | C= O stretching of amide I |
| - | 1451.51 | 1373 | Amino II (-NH2) |
| 1132.08 1072.30 1001.27 | 1131.04 1070.40 1000.16 | 1126.99 1069.85 1001.83 | P–O stretching |
| 897.48 | 894.49 | 896.14 | P–O(H) stretching |
| 575.09 | 565.54 | 563.59 | O–P–O(H) bending mode |

|  | Element; Wt %; At %. C K; 4.68; 9.63. O K; 29.75; 46.02. Na K; 0.17; 0.18. P K; 21.23; 16.94. Ca K; 44.17; 27.23. Total; 100; 100. |
| --- | --- |

S3 SEM  images and EDX analysis of (DCP)

|  | Element; Wt %; At %. C K; 8.04; 14.73. N K; 3.23; 3.13. O K; 30.21; 45.02. Na K; 0.31; 0.32. P K; 17.04; 13.22. Ca K; 41.17; 23.58. Total; 100; 100. |
| --- | --- |

S4 SEM images and EDX analysis of (DCP-CS2)

|  | Element; Wt %; At %. C K; 5.53; 11.55. O K; 27.97; 43.84. Na K; 0.10; 0.11. P K; 20.17; 16.33. Ca K; 41.92; 26.23. Fe K; 4.31; 1.93. Total; 100; 100. |
| --- | --- |

S5 SEM images and EDX analysis of (DCP) after (Fe2+) ions uptake

|  | Element; Wt %; At %. C K; 9.59; 19.63. N K; 3.11; 3.10. O K; 23.16; 36.06. Na K; 0.31; 0.33. P K; 17.34; 13.56. Ca K; 41.33; 25.05. Fe K; 5.16; 2.27. Total; 100; 100. |
| --- | --- |

S6 SEM images and EDX analysis of (DCP-CS1) after (Fe2+) ions uptake

|  | Element; Wt %; At %. C K; 9.82; 20.28. N K; 3.24; 3.21. O K; 27.14; 40.47. Na K; 0.37; 0.38. P K; 16.79; 12.31. Ca K; 38.62; 21.65. Fe K; 4.02; 1.70. Total; 100; 100. |
| --- | --- |

S7 SEM images and EDX analysis of (DCP-CS2) after (Fe2+) ions uptake

S8 Effect the dose of (DCP) and (DCP-CS1) at 120 min., (DCP-CS2) at 60 min. on (Fe2+) ions , initial concentration of 100 mgL-1, natural pH of 4.9 at temperature 25±1oC

S9 Effect the dose of (DCP) on the (Fe2+) ions Adsorption

| S.NO. | Adsorbent dose (mg) | C e (mg/L) | Amount adsorbed, q (mg/g) | Removal % of (Fe2+) ions |
| --- | --- | --- | --- | --- |
| 1 | 20 | 60 | 20 | 40 |
| 2 | 40 | 38 | 15.5 | 62 |
| 3 | 60 | 25 | 12.5 | 75 |
| 4 | 80 | 21.33 | 9.83 | 78.67 |
| 5 | 100 | 12.5 | 8.75 | 87.5 |

S10 Effect the dose of (DCP – CS1) on the (Fe2+) ions Adsorption

| S.NO. | Adsorbent dose (mg) | C e (mg/L) | Amount adsorbed, q (mg/g) | Removal % of (Fe2+) ions |
| --- | --- | --- | --- | --- |
| 1 | 20 | 58 | 21 | 42 |
| 2 | 40 | 40 | 15 | 60 |
| 3 | 60 | 24 | 12.6 | 76 |
| 4 | 80 | 20 | 10 | 80 |
| 5 | 100 | 12 | 8.8 | 88 |

S11 Effect the dose of (DCP – CS2) on the (Fe2+) ions Adsorption

| S.NO. | Adsorbent dose (mg) | C e (mg/L) | Amount adsorbed, q (mg/g) | Removal % of (Fe2+) ions |
| --- | --- | --- | --- | --- |
| 1 | 20 | 36 | 32 | 64 |
| 2 | 40 | 15.33 | 21.16 | 84.67 |
| 3 | 60 | 12.66 | 14.55 | 87.34 |
| 4 | 80 | 12.66 | 10.91 | 87.34 |
| 5 | 100 | 8 | 9.2 | 92 |

S12 Effect of contact time on (Fe2+) ions adsorption (pH=4.9) from solutions under conditions of (DCP), (DCP-CS1) and (DCP-CS2) mass 100 mg/10 mL, 50 mg/L (Fe2+) ions concentration at temperature 25±1oC

S13 Equilibrium Data for (Fe2+) ions removal by (DCP) at Different Times

| S.NO. | Contact Time / minutes | C e (mg/L) | Amount adsorbed, q (mg/g) | Removal % of (Fe2+) ions |
| --- | --- | --- | --- | --- |
| 1 | 1 | 41.25 | 0.875 | 17.5 |
| 2 | 2 | 37.6 | 1.240 | 24.8 |
| 3 | 5 | 27.25 | 2.275 | 45.5 |
| 4 | 10 | 23 | 2.70 | 54 |
| 5 | 15 | 19.25 | 3.075 | 61.5 |
| 6 | 20 | 12 | 3.80 | 76 |
| 7 | 25 | 10 | 4 | 80 |
| 8 | 30 | 7 | 4.30 | 86 |
| 9 | 40 | 4.50 | 4.55 | 91 |
| 10 | 50 | 3.75 | 4.625 | 92.5 |
| 11 | 60 | 2.80 | 4.720 | 94.4 |
| 12 | 70 | 2.33 | 4.767 | 95.34 |
| 13 | 80 | 2.33 | 4.767 | 95.34 |
| 14 | 100 | 2.33 | 4.767 | 95.34 |

S14 Equilibrium Data for (Fe2+) ions removal by (DCP – CS1) at Different Times

| S.NO. | Contact Time / minutes | C e (mg/L) | Amount adsorbed, q (mg/g) | Removal % of (Fe2+) ions |
| --- | --- | --- | --- | --- |
| 1 | 1 | 40 | 1 | 20 |
| 2 | 2 | 34.75 | 1.525 | 30.5 |
| 3 | 5 | 22 | 2.8 | 56 |
| 4 | 10 | 18.5 | 3.15 | 63 |
| 5 | 15 | 14.1 | 3.59 | 71.8 |
| 6 | 20 | 10 | 4 | 80 |
| 7 | 25 | 7.75 | 4.22 | 84.5 |
| 8 | 30 | 6 | 4.40 | 88 |
| 9 | 40 | 4 | 4.60 | 92 |
| 10 | 50 | 3.25 | 4.675 | 93 |
| 11 | 60 | 2.55 | 4.745 | 94.9 |
| 12 | 70 | 2 | 4.8 | 96 |
| 13 | 80 | 2 | 4.8 | 96 |
| 14 | 100 | 2 | 4.8 | 96 |

S15 Equilibrium Data for (Fe2+) ions adsorption by (DCP – CS2) at Different Times

| S.NO. | Contact Time / minutes | C e (mg/L) | Amount adsorbed, q (mg/g) | Removal % of (Fe2+) ions |
| --- | --- | --- | --- | --- |
| 1 | 1 | 35.5 | 1.45 | 29 |
| 2 | 2 | 29 | 2.1 | 42 |
| 3 | 5 | 19.5 | 3.05 | 61 |
| 4 | 8 | 13 | 3.70 | 74 |
| 5 | 10 | 10.5 | 3.95 | 79 |
| 6 | 12 | 9 | 4.1 | 82 |
| 7 | 15 | 7 | 4.3 | 86 |
| 8 | 20 | 5.5 | 4.45 | 89 |
| 9 | 25 | 4.75 | 4.525 | 90.5 |
| 10 | 30 | 3.75 | 4.625 | 92.5 |
| 11 | 40 | 3 | 4.7 | 94 |
| 12 | 50 | 2.25 | 4.775 | 95.5 |
| 13 | 60 | 1.33 | 4.867 | 97.34 |
| 14 | 70 | 1 | 4.9 | 98 |
| 15 | 80 | 1 | 4.9 | 98 |

S16: Effect of intial concentration on the adsorption of (Fe2+) ions at pH= 4.9, from solution by (DCP), (DCP-CS1) and (DCP-CS2) under conditions of mass 100 mg/10 mL at 120 min. and temperature of 25±1oC

S17 Initial (Fe2+) ions metal concentration effect on (DCP) adsorption Mechanism

| S.NO. | C 0 (mg/L) | C e (mg/L) | Amount adsorbed, q (mg/g) | Removal % of (Fe2+) ions |
| --- | --- | --- | --- | --- |
| 1 | 25 | 1.13 | 2.38 | 95.48 |
| 2 | 50 | 2.33 | 4.76 | 95.34 |
| 3 | 100 | 12.5 | 8.75 | 87.5 |
| 4 | 150 | 39 | 11.1 | 74 |
| 5 | 200 | 88 | 11.2 | 56 |
| 6 | 250 | 113.33 | 13.66 | 54.66 |

S18 Initial (Fe2+) ions metal concentration effect on (DCP – CS1) adsorption Mechanism

| S.NO. | C 0 (mg/L) | C e (mg/L) | Amount adsorbed, q (mg/g) | Removal % of (Fe2+) ions |
| --- | --- | --- | --- | --- |
| 1 | 25 | 0.73 | 2.43 | 97.08 |
| 2 | 50 | 2 | 4.8 | 96 |
| 3 | 100 | 12 | 8.8 | 88 |
| 4 | 150 | 33.99 | 11.60 | 77.34 |
| 5 | 200 | 73.33 | 12.67 | 63.34 |
| 6 | 250 | 101.66 | 14.83 | 59.34 |

S19 Initial (Fe2+) ions metal concentration effect on (DCP – CS2) adsorption Mechanism

| S.NO. | C 0 (mg/L) | C e (mg/L) | Amount adsorbed, q (mg/g) | Removal % of (Fe2+) ions |
| --- | --- | --- | --- | --- |
| 1 | 25 | 0.23 | 2.48 | 99.08 |
| 2 | 50 | 1.33 | 4.86 | 97.34 |
| 3 | 100 | 8 | 9.2 | 92 |
| 4 | 150 | 13.99 | 13.60 | 90.67 |
| 5 | 200 | 28 | 17.2 | 86 |
| 6 | 250 | 65 | 18.5 | 74 |

S20 Pseudo-first-order of (Fe2+) ions (pH=4.9), adsorbed on (DCP), (DCP – CS1) and(DCP – CS2) at conditions of 50 mg/L metal ions concentration, mass 100 mg/10 mL at 25±1oC

S21 Experimental and calculated parameters of pseudo-first and second order kinetic of (Fe2+) ions (natural pH of 4.9) on (DCP), (DCP – CS1) and (DCP – CS2)

| Kinetic parameters Adsorpent | qe experimental | Pseudo- first- order |  |  | Pseudo- second- order |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  |  | qe calculated | K1 | R2 | qe calculated | K2 | R2 |
| DCP | 4.767 | 3.7899 | 0.07195 | 0.99177 | 5.2929 | 0.02519 | 0.99299 |
| (DCP – CS1) | 4.8 | 3.3498 | 0.0691 | 0.99048 | 5.0836 | 24.5061 | 0.9993 |
| (DCP – CS2) | 4.9 | 2.3097 | 0.06752 | 0.9466 | 5.0831 | 0.067421 | 0.99991 |